## Slide 1: LPT 606: SLAUGHTER HOUSE BYPRODUCTS TECHNOLOGY (2+1) UNIT III – Processing of hide and skin for preparation of leather
Dr. R. K. Jaiswal
Asstt. Prof.-cum-Jr. Scientist
Dept. of Livestock Products Technology
Bihar Veterinary College
Bihar Animal Sciences University
Patna-800014 (Bihar)

## Slide 2: Hide and Skin
Animal hide contributes a significance proportion 4-11% of live
animal weight and a valuable animal by products.
Cost of hide/skin can fetch 55-60% of byproduct value.
“Skin” term is used for small hides, and in cattle this indicates
a weight of less than 13.62 kg after curing.
Hide: Skin obtained from fully grown large animal (more than
13.62 kg after curing)
Large
Thick
Heavy
Skin: Integral body covering of sheep, goat, pig and young calf.
In tannery hide and skin are converted into leather

## Slide 3: Processing of hide and skin
The leather manufacturing process is divided into 3 sub- processes: Preparatory stages and Tanning and Crusting.
All true leathers will undergo these sub-processes.
A further sub-process, surface coating may be added into the sequence.
The list of operations that leathers undergo vary with the type of leather.
The leather making process is in general restricted to batch processing, but if the surface coating sub-process is added then some continuous processing can be included.
The operation flow has to follow, the preparatory → tanning → crusting → surface coating sub-process order without deviation, but some of the sub-processes can be omitted to make certain leathers (or partially tanned/untanned products).

## Slide 4
Processing of hide/skin begins with obtaining an animal skin, the animal
is killed and skinned before the body heat leaves the tissues.
This can be done by the tanner, or by obtaining a skin at a
slaughterhouse, farm, or local fur trader.
Skinning operation is called flaying, performed by skilled workers
following a uniform pattern.
  Done on pritch plate: Steel plate (diameter 20 cm, 120 cm length, 60 cm width), Anchored with bolt to floor.
  Enough watering at antemortem facilitates flaying.
  Hoisting of animal improves bleeding, good keeping quality of hide
Types flaying:
Knife Skinning- With conventional skinning knives
- Air driven reciprocating skinning knives
Hide pulling - Using hide puller
Hide separation- Pumping compressed air into carcass

## Slide 5: A. Preparatory stages
The preparatory stages are when the hide/skin is prepared for tanning.
During the preparatory stages many of the unwanted raw skin
components are removed.
Many options for pretreatment of the skin exist, not all of the
options may be performed.
Preparatory stages may include,
-Preservation- the hide/skin is treated with a method mainly
curing which renders it temporarily imputrescible.
Preparing hides begins by curing them with salt.
Curing is employed to prevent putrefaction of the protein substance (collagen) from bacterial growth during the time lag from procuring the hide to when it is processed.
Curing

## Slide 6
Curing removes water from the hides and skins using a
difference in osmotic pressure.
The moisture content of hides and skins is greatly reduced, and osmotic pressure increased, to the point that bacteria are unable to grow.
In dry-salting/curing, the hides are heavily salted, then pressed into packs for about 30 days.
In brine or wet-curing, the hides are agitated in a saltwater
bath for about 16 hours.
Curing can also be accomplished by preserving the hides
and skins at very low temperatures.

## Slide 8: Beamhouse operations
The steps in the production of leather between curing and tanning are collectively referred to as beamhouse operations.
This include, in order,
  Soaking,
  Liming,
Removal of fleshing),
Deliming,
Bating
extraneous tissues (unhairing, scudding and
Drenching, and
Pickling.

## Slide 10: Soaking
Soaking is carried out to allow hides and skins to reabsorb any water which may have been lost after flaying, in the curing process, or during transport.
Soaking also cleans the hides and skins (removal of dung, blood, dirt, etc.) and removes interfibrillary material so that the hide or skin can be further treated.
The soaking methods used depend on the state of the hides. The process is mostly carried out in two steps: a dirt soak to remove the salt and dirt, and a main soak.
The duration of soaking can range from several hours to a
few days.
Putrefying bacteria can thrive during soaking and biocides
may be added to curtail their activity.

## Slide 11
To prevent damage of the skin by bacterial growth during the soaking period, biocides, typically dithiocarbamates, is be used.
Fungicides such as 2-thiocyanomethylthiobenzothiazole is also be added later in the process, to protect wet leathers from mold growth.
The use of pentachloro phenol and mercury-based biocides
and their derivatives is forbidden
Depending on the type of raw materials being soaked, other additives may be used, such as surfactants and enzyme preparations.

## Slide 12: Liming
After soaking, the hides and skins are taken for liming: treatment with milk of lime (a basic agent, pH-11-12) that may involve the addition of "sharpening agents" (disulfide reducing agents) such as sodium sulfide, cyanides, amines, etc.
The objectives of this operation are mainly to:
  Remove some of the interfibrillary soluble proteins such as mucins.
  Remove the hair and other keratinous matter.
  Swell up and split up the fibres to the desired extent.
  Remove the natural grease and fats to some extent.
  Bring the collagen in the hide to a proper condition for satisfactory tannage

## Slide 13
The interfibrillary
proteins are denatured by the
presence of alkali, rendered soluble, facilitating their removal from the leather.
Failure to remove these proteins results in a hard, tinny leather (due to fibre glueing upon drying) that is brittle and inflexible.
Keratin that is present in the hair, scales and in the epidermis of the skin is hydrolyzed in the presence of alkali.
The disulfide bridges found in keratin protein are cleaved.
Long periods of liming will result in hair removal.
The main removal of keratin is performed during the
unhairing operation.
In traditional processing, liming and unhairing are indivisible
and take place at the same time.

## Slide 14
The presence of calcium hydroxide results in the alkaline
swelling of skin.
The result is an influx of water into the hide/skin, and a marked increase in fibre diameter.
The thickness of the skin increases, but the surface area of
the pelt decreases.
The weight increase, owing to the uptake of water, results
in a doubling of the hide/skin weight.
The action of liming, in particular the swelling of the skin,
results in the splitting of the fibre bundle sheath.
Owing to the fibre diameter increasing, the bundle sheath
cannot contain the thicker fibres.
This allows increased access to the fibres, which allows
better tanning, retanning, dyeing and fatliquoring.

## Slide 15: Unhairing and scudding
Unhairing agents used at this time include sodium sulfide, sodium hydroxide, sodium hydrosulfite, calcium hydrosulfide, dimethyl amine, and sodium sulfhydrate.
The majority of hair is then removed mechanically, initially with a machine and then by hand using a dull knife, a process known as scudding.

## Slide 16: Deliming and bating
The pH of the collagen is brought down to a lower level so the
enzymes may act on it, in a process known as deliming.
Depending on the end use of the leather, hides may be treated with enzymes to soften them, a process called bating. Additional removal of protein material loosened by liming is achieved by enzymatic digestion- the operation of bating.
In modern tanning, these enzymes are purified agents, and the process no longer requires bacterial fermentation (as from dung-water soaking) to produce them.
Two main types: Pancreatic bates: digestive enzymes from pancreatic glands, Bacterial bates: digestive enzymes of bacteria.

## Slide 17
Method of bating:
The hides and skins are delimed to a pH of 8.0-8.5 and washed. This is the degree of alkalinity at which most enzymes show greatest digestive power.
The goods are then usually treated in 300-500% water at 37°C with a 1-2% addition of the powdered enzyme mixture. It is important to maintain the pH and temperature accurately, as slight variations give great loss of bating power.
When slight flattening of the grain or increase in flexibility is
required the time of bating is short (1 hr).
Longer bating times are necessary for extreme stretch and
suppleness.
The digestive action of bating is stopped by making conditions unsuitable for enzyme activity by cooling to 16°C.

## Slide 18: Pickling
Once bating is complete, the hides and skins are treated first with common salt (sodium chloride) and then with sulfuric acid, in case a mineral tanning is to be done.
Pickling is carried out at 30-37°C tem to reduce the pH of the pelt prior to mineral tanning and some organic tannages (e.g. chrome tanning, glutaraldehyde tanning, and vegetable tanning), thereby sterilising the skin, ending the bating action, and improving the penetration of the subsequent tanning material.
This is done to bring down the pH (medium is kept at around 3.5) of collagen to a very low level so as to facilitate the penetration of mineral tanning agent.
The salt penetrates the hide twice as fast as the acid and
checks the ill effect of sudden drop of pH.

## Slide 19: B. Tanning
Tanning is the process that converts the protein of the raw hide or skin into a stable material which will not putrefy and is suitable for a wide variety of end applications.
The principal difference between raw hides and tanned hides is that raw hides dry out to form a hard inflexible material that can putrefy when re-wetted (wetted back), while tanned material dries out to a flexible form that does not become putrid when wetted back.
The most commonly used tanning material is chromium, which leaves the leather, once tanned, a pale blue colour (due to the chromium), this product is commonly called “wet blue”

## Slide 20
Leather tanning is the
process of converting raw
hides or skins into leather.
Hides and skins have the ability to absorb tannic acid and other chemical substances that prevent them from decaying, make them resistant to wetting, and keep them supple and durable.
The surface of hides and skins contains hair and oil glands and is known as grain side. The flesh side of the hide or skin is much thicker and softer.
The three types of hides and skins most often used in
leather manufacture are from cattle, sheep and goat.

## Slide 21
Tanning is essentially the,
Reaction tannins, agents.
of collagen
fibers
in the hide with
chromium, alum, or other chemical
The most common tanning agents used are trivalent chromium and vegetable tannins extracted from specific tree barks.
Alum, syntans (man-made chemicals), formaldehyde, glutaraldehyde, and heavy oils are other tanning agents.

## Slide 22: Chrome tanning
Chromium (III) sulfate ([Cr(H2O)6]2(SO4)3) has long been regarded
as the most efficient and effective tanning agent.
Chromium(III) sulfate dissolves to give the hexa-aqua-chromium(III) cation, [Cr(H2O)6]3+, which at higher pH undergoes processes called olation to give polychromium (III) compounds that are active in tanning being the cross-linking of the collagen subunits.
Collagen's high content of hydroxyproline allows for significant cross-linking by hydrogen bonding within the collagen helical structure.
Ionized carboxyl groups (RCO2−) are formed by hydrolysis of the collagen by the action of hydroxide during the liming process, before introduction of the tanning agent (chromium salts).
The ionized carboxyl groups coordinate as ligands to the chromium(III) centers.
Tanning increases the spacing between protein chains in collagen from 10 to 17 Å.

## Slide 23
Prior to the introduction of the basic chromium species in tanning, several steps are required to produce a tannable hide.
The pH must be very acidic when the chromium is introduced to ensure that the chromium complexes are small enough to fit in between the fibers and residues of the collagen.
Once the desired level of penetration of chrome into the substance is achieved, the pH of the material is raised again to facilitate the process, this step is known as basification.
In the raw state, chrome tanned skins are greyish-blue, so are
referred to as wet blue.
Chrome tanning is faster than vegetable tanning and produces a stretchable leather which is excellent for use in handbags and garments.

## Slide 24
Subsequent to application of the chromium agent, the bath is treated with sodium bicarbonate to increase the pH to 4.0–4.3, which induces cross-linking between the chromium and the collagen.
The pH increase is normally accompanied by a gradual
temperature increase up to 40 °C.
Chromium-tanned leather can contain between 4 and 5%
of chromium.
This efficiency is characterized by its increased hydrothermal stability of the skin, and its resistance to shrinkage in heated water.

## Slide 25: Vegetable tanning
Vegetable tanning uses tannins (a class of polyphenol astringent chemicals), which occur naturally in the bark and leaves of many plants.
Tannins bind to the collagen proteins in the hide and coat them, causing them to become less water-soluble and more resistant to bacterial attack.
The process also causes the hide to become more flexible.
The primary barks processed in bark mills and used in modern times are chestnut, oak, redoul, tanoak, hemlock, quebracho, mangrove, wattle (acacia).
Hides are stretched on frames and immersed for several
weeks in vats of increasing concentrations of tannin.
Vegetable-tanned hide is not very flexible and is used for luggage, furniture, footwear, belts, and other clothing accessories.

## Slide 26: C. Crusting
Crusting is the process of thinning, retanning and
lubricating the hide/skin is.
Often a coloring operation is included in the crusting sub-
process.
The chemicals added during crusting have to be fixed in
place.
The culmination of the crusting sub-process is the drying and softening operations.
Crusting may include the following operations:
  Tawing, Splitting, Skiving, Sorting, Neutralizing, Filling out, Dyeing, Greasing/Oiling, Drying, Staking, Finishing:

## Slide 27: Tawing
Tawing is a method of soaking tanned skin to warm (20-30
°C) potash alum and aluminium salts solution, in conjunction with egg yolk, flour, and other salts to increases the leather's pliability, stretchability, softness, and quality.
Then, the leather is air dried (crusted) for several weeks, which allows it to stabilize.
However, exposure and aging may cause slight yellowing over time and, if it remains in a wet condition, tawed leather will suffer from decay.
Tawing is traditionally used on pigskins and goatskins to
create the whitest colors

## Slide 28
Splitting: In order to achieve an even specified thickness the leather is reduced in
The resulting
can than be
further
as
substance. split-leather processed suede.
Skiving: The grain leather is brought to an even thickness. Irregularities are removed from the reverse side and the leather is separated into color-batches.
Sorting: The leather is sorted into various quality grades.

## Slide 29
Neutralizing,
Dyeing
Oiling/Greasing:
and
The acid
tanning
resulting from the process
is neutralized,
then
Dyeing takes
place,
where
appropriate with anilin-dye-
stuffs. The greasing procedure
will finally achieve the correct
softness.
Drying: Two methods are used to
dry leather. The vacuum process
during which moisture is
removed by suction and the
hanging process, when leather is hung and taken through ovens.
Staking: Following drying the
leather is mechanically staked in
order to soften it. Further
processes take place in
preparation for finishing.

## Slide 30
Finishing:
Here the leather is given its final surface treatment and look, through processes of base coat, coloring, embossing, ironing the leather becomes, matt or shiny, two-tone or uni-colored, smooth or grained. (as per demands of fashion).
The art of finishing lies in working in wafer-thin layers without disturbing the natural look of the leather and its characteristics such as suppleness and breathability.