## Slide 1: Packaging

## Slide 2: Packaging
It refers to wrapping or covering any items including food to protect from damage / spoilage and present aesthetic look.
Packaging of food items are used to extend the keeping quality and minimize contamination.

## Slide 3: Function of Packaging
Primarily functions for packaging as follows.
  To contain the product
  To protect (and preserve) the product
  To present the product to the consumer in attractive way
As a container in which fast foods may be heated or in which hot foods may be deposited (as in the case of a plate)Some important factors to be considered for the type of packaging material to be used in the food are,
  the raw material used for packaging is easily available and economically viable
  the material should withstand the stress and strain of machineries which often operate at high speeds.
The package must not have any adverse effects on the contents and must comply with all legal requirements. Also, due consideration should be given to the ultimate disposal of packaging materials and their effect on environment.

## Slide 4: Plastics for packaging
Plastics are widely used for the manufacture of flexible packaging materials like films, semi rigid and rigid containers such as jars and bottles. The important plastic materials used in packaging are.

## Slide 5: Plastics for packaging
The important plastic materials used in packaging are.
Ethylenic Thermoplastics or Vinyl Plastic or Polyolefins:
  PE (LDPE, LLDPE & HDPE)
  EVA
  Ethylene propylene copolymers
  PP
  Vinyl Plastics
  PVC
  VDC
  PVDC
  Ethylene Vinyl alcohol Copolymer (EVOH)
  PTFE
  Polystyrene
  EPS

## Slide 6: Plastics for packaging
Nonethylenic Thermoplastics (Condensation polymers)
  Polyester or Polyethylene terephthatate (PET)
  PA
Regenerated cellulose film

## Slide 7: Ethylenic Thermoplastics
Most of the thermoplastics are derevatives of ethylene.
They are also known as Vinyl Plastic or polyolefins.
Ethylenic polymers used in plastic.

## Slide 8: Polyethylene (CH2CH2)
PE is consumed in the largest quantity by the packaging industry.
Made by polymerisation of ethylene (natural state gas).
Polymerisation under very high pressure (1200 atm) and high temperature (150 - 200˚C) in presence of traces of oxygen yields a macromolecules with very high degree of branching _ LDPE.

## Slide 9: LDPE
The most widely used plastic for food packaging films.
  LDPE is strong, slightly translucent flexible material possessing excellent resistance to most chemical below 60˚C.
  Relatively low cost
  Fairly tough (good mechanical strength properties such as tensile, burst, impact and tear strength)
  Ease of heat sealing and good seal strength.
  Good barrier against water vapour but not so good against oxygen and other gases.
  Good low temperature resistance.
  Subjected to stress cracking in presence polar chemicals.
  LDPE is soluble in hydrocarbon and chlorinated hydrocarbon solvent.

## Slide 10: Limitations of LDPE
Not completely clear (Slight haze) can sometimes be a slight disadvantage for display type packages.
Softens at 90˚C, thus it is not suitable for steam sterilization, boil-in bag or ovenable pack applications.
It is not a good oxygen barrier compared to other plastics.
Does not have good resistance to grease or oil.

## Slide 11: Linear Low density polyethylene (LLDPE)
At low pressure forms polymers with long parallel linear chains _ LLDPE.
This has an extremely high tensile strength and very high stretch with very good heat sealing characteristics.
Used for heavy duty sacks and stretch wrap applications.
It is used for incorporating into HDPE to reduce brittleness and increase tensile strength of carry bags.

## Slide 12: High density Polyethylene (HDPE)
HDPE is produced using a low temperature (60-160˚C) and low pressure process employing alkyl metal catalyst in the process.
It is stiffer, harder and less transparent but possesses greater resistance to oils and grease.
It offers excellent moister protection and has higher softening point but the impact resistance is low.

## Slide 13: High density Polyethylene (HDPE)
HDPE gives a stiffer film than LDPE and has higher barrier properties to water vapour and gases by a factor of around 5.
Because of extra stiffness and strength, HDPE can be used as a very thin film, eg : 10 µm, when it is similar to grease proof tissue paper, it is water proof and hence used for butcher wrappings.
As it is tough, it is used for making super market carry bags. As HDPE does not soften at 100oC, it may be used in the manufacture of boil-in-bag type packages.

## Slide 14: Polypropylene (PP)
Polymerization of propylene, employing stereospecific catalyst & low pressure.
Properties of PP:
  More rigid, stronger and lighter than PE.
  Harder and higher softening point than HDPE.
  Greater resilience, good gloss.
  Greater resistance to chemical except hot aromatic and chlorinated hydrocarbon solvents.
  Low water vapour permeability.
  Good grease resistance.
  Lower shock resistance at lower temperatures.
  Stable at high temperatures.
  Can take on print without difficulty.

## Slide 15: Polypropylene (PP)
PP is generally used in the oriented forms.
Biaxially-oriented PP (BOPP) films i.e. the film stretched in two direction at right angle under suitable temp.
Have improved gloss & clarity, tensile strength, abrasion and barrier properties against WV & Oxygen.
uits.

## Slide 16: Vinyl Plastics
Polyvinyl Chloride (PVC)
  Polymer of vinyl chloride (CH2CHCl) i.e. ethylene in which one H-atom is substituted by a chlorine.
  It is hard, stiff, clear glossy material with excellent moisture resistance and low gas permeability.
  By addition of plasticiser flexible films can be obtained.
  Maximum residual monomer limit is 1 mg/kg due to its carcinogenic nature.
  Highly plasticized PVC is used as a cling film for over wrapping super market trays of fresh produce such as red meat, poultry fresh fruits and vegetable and cheese.

## Slide 18: Polyvinyl Chloride (PVC)

## Slide 19: Vinylidene Chloride
CH2CCl2.
It is hard solid with high degree of crystallinity.
Insoluble in most solvents
Have very low water absorption.
The film produce is clear with very low permeability to vapours.

## Slide 20: Polyvinylidine (PVDC)
Produced as a copolymer with 13-20% vinyl chloride and vinylidine chloride .
It contains a low percentage of plasticisers, slip agents and stabilisers. These films are clear.
Have excellent mechanical resistance
Extremely low water vapor permeability
Extremely low oxygen permeability
Suitable for heat sealing
Very expensive.

## Slide 21: Polyvinylidine (PVDC)
Widely used as a very thin barriers coating on other material, eg. Cellulose film, poly propylene and paper for the packaging of moisture sensitive foods.

## Slide 22: Polytetrafluroethylene (PTFE)
Polymer of ethylene C2F4.
It is highly crystalline.
Has High Mol. Weight and is smooth and waxy.
It can produce non-stick surface and withstand high temperatures.

## Slide 23: Polystyrene (PS)
Styrene is ethylene where one H-atoms is substituted by a phenyl redical, CH2-CH-C6H5.
It is amorphous and brittle in nature, colourless and transparent unless pigmented.
Good barrier against gases but not against water vapour.
Soluble in number of solvents.
Softens at 85 to 95oC.
The addition synthetic butadiene or polybutadiene to polystyrene improve the impact strength and such material is referred as High Impact PolyStyrene (HIPS).

## Slide 24: Polystyrene (PS)
Used for screw caps especially polyethylene bottles.
Toughened grades (HIPS) high impact polystyrene are used in making tubs or pots for products such as yoghurt, dairy cream, glazed cherries etc.,

## Slide 25: Expanded polystyrene (EPS)
Produced by mixing PS heads with 5 to 7% blowing agent such as pentene or chlorofluorocarbon and steam heating at 95oC.
PS begins to soften and blowing agent is released from the solid solution causing rapid expansion of the beads giving a cellular structure.
EPS is an excellent heat insulator used for containers for hot take away foods or for boxes for transporting fresh (iced) fish.
They are also used for packing where cushioning is required (Eg. egg trays or fruit or tomato) or as cushioning materials.

## Slide 27: Ethylene Vinyl alcohol Copolymer (EVOH)
Higher water vapour barrier than polyolefins
Extremely low oxygen permeability, in the absence of moisture
High oil resistance
Very expensive
Its outstanding gas barrier properties enable it to be used for packaging foods sensitive to oxygen but it must be protected from ingress of moisture by laminating with LLDPE-Water barrier / EVOH-Gas barrier / LLDPE-Heat sealing medium.

## Slide 28: Condensation polymers
Polyester or Polyethylene terephthatate (PET)
  This was first developed as a textile fibre by I.C.I Ltd., Later it was developed to form film and for bottle by stretch below moulding.
Important properties of PET are:
  High tensile strength and therefore withstands carbon dioxide pressure in bottles.
  High softening point i.e. 245-270oC, but the jars/bottles suffer from distortion on hot filling.
  It has good sparkle and optical clarity.
  Good gas barrier, better than PVC and polyolefins (PE&PP). Hence used in Modified Atmosphere Packaging (MAP), Gas Packaging and Vacuum packaging.
  Fairly low water vapor permeability.
  Excellent oil and grease resistance.
  Chemical resistance to dilute acids and alkalies but attacked by concentrated areas.

## Slide 29
Excellent Printing Surface: PET bottles up to 3L capacity are widely used for carbonated drinks where its gas barrier properties and strengths are valuable.
As a film difficult to heat seal (high M.P) and thus coated with PVDC or laminated to polyethylene.
Such laminates are used in vacuum packaging of cooked meat products, and for boil in bag packs.
More recent use for PET is in the manufacture of ovenable boards for heating in microwave or conventional hot air ovens.
By laminating with other plastics it is also used in the manufacture of retortable pouches and pouches for MAP products.

## Slide 31
Thank You